## Slide 1
Multi-Scale Computational Approaches for Materials Property Prediction and Design
Manh Tien Nguyen

## Slide 2
DFT
Catalytic piperidine +CO2
SrO and Sr(OH)2.nH2O + CO2
MD
Ionic Solvation and Transport in Zwitterionic Electrolytes
ML
Deep Learning Potential for CO2+deep eutectic solvents reactions
Finding reaction pathways
Material Design

## Slide 3
A novel catalytic method for low-energy CO2 capture
Samir Budhathoki a, Manh Tien Nguyenb, Qinghua Lai c, Xuejing Kanga, Sean X. Tanga,
Zhe Chena, Kevin Jayaatmajac, Ramhari Panerua, Hertanto Adidharmac, Yuhua Duanb*,
Maohong Fan d,e*
a Department of Energy & Petroleum Engineering, University of Wyoming, Laramie, WY 82071, USA
b National Energy Technology Laboratory, United States Department of Energy, Pittsburgh, PA, 15236, USA
c Department of Chemical & Biomedical Engineering, University of Wyoming, Laramie, WY 82071, USA
d College of Engineering and Physical Science, and School of Energy Resources, University of Wyoming, Laramie,
WY, 82071, USA
eCollege of Engineering, Georgia Institute of Technology, Atlanta, GA 30332, USA

## Slide 4
Free energy profiles and reaction pathways. Pathway I/Bicarbonate for catalyzed and uncatalyzed pathway II for aqueous piperidine sorbent.
Computed profiles show that CCAF ease the reaction pathway
Single reaction pathway
Yields the formation of HCO3- and R-NH2+
aluminum formate-water-piperidine complex

## Slide 5
Free energy profiles and reaction pathways. Pathway II/ZW mechanism for catalyzed and uncatalyzed pathway II for aqueous piperidine sorbent.
Pathway II (Zwitterion mechanism)
(Overall reaction)
(Zwitterion/ZW)

## Slide 6
(a). Step 1: CO2 not reacted
(b). Step 2: Transition state 1
Energy: 0.00 eV
(c). Step 3: Final state
Rxn: R-NH + CO2 + H2O
(a). Uncatalyzed pathway I (HCO3-)
Energy: 0.49 eV
Rxn: HCO3- RNH2+
Energy: 0.02 eV
Rxn: HCO3- + RNH2+
(b). Step 2: Transition state 1
Energy: 0.00 eV
(c). Step 3: Final State
Rxn: R-NH + CO2 + H2O with CCAF
(b).Catalyzed Pathway I (HCO3-)
Energy: 0.39 eV
Energy: -0.24 eV
Rxn: HCO3- + RNH2+ with CCAF
(a). Step 1: CO2 not reacted
Rxn: HCO3- RNH2+ with CCAF

## Slide 7
(a). Step 1: CO2 not reacted
(b). Step 2: Transition state 1
Energy: 0.00 eV
Energy: 0.19 eV
(c). Step 3: Intermediate product
Energy: 0.18 eV
(d). Step 4: Initial intermediate product
(f). Step 6: Final state
(e). Step 5: Transition state 2
Energy: 0.18 eV
Energy: 0.31 eV
Energy: 0.13 eV
Rxn: R-NH + CO2
Rxn: R-NH+-CO2
Rxn: R-NH+COO-
Rxn: R-NCOO- + RNH2+
Rxn: R-NCOO- R-NH2+
Rxn: R-NH+COO- R-NH
(c).Uncatalyzed Pathway II (R-NCOO-)
(a). Step 1: CO2 not reacted
(b). Step 2: Transition state 1
Energy: 0.00 eV
Energy: 0.13 eV
(c). Step 3: Intermediate product
Energy: -0.02 eV
(d). Transition state 2
(f). Step 6: Final state
(e). Transition state 3
Energy: 0.08 eV
Energy: -0.07 eV
Energy: -0.14 eV
Rxn: 2R-NH + CO2 with CCAF
Rxn: R-NH+-CO2 + R-NH with CCAF
Rxn: R-NH+COO- + R-NH with CCAF
Rxn: R-NCOO- + RNH2+ with CCAF
Rxn: R-NCOO- R-NH2+ with CCAF
Rxn: R-NH+COO- R-NH with CCAF
(d). Catalyzed Pathway II (R-NCOO-)

## Slide 8: Theoretical study of CO2 capture mechanisms of SrO and Sr(OH)2.nH2O (n=0,1,8)
Manh Tien Nguyen, Dominic Alfonso, Christopher M. Marin, Douglas Kauffman, Yuhua Duan
National Energy Technology Lab

## Slide 9: CO2 Capture using SrO
9
Reactive capture uses metal oxides and solid carbon to capture/convert CO2
Capture: Thermally heating a mixture of CO2 and metal oxide forms a stable metal carbonate:
CO2 + MO → MCO3
Conversion: Subsequently heating the MCO3 and solid carbon produces carbon monoxide and regenerates the sorbent
1. MCO3 + C → 2CO + MO (commercially useful)
2. MCO3 → CO2 + MO
CaO has been used due to relatively low-cost and abundance
SrCO3/SrO showed much better CO selectivity than CaCO3/CaO
Wang, N., Feng, Y., & Guo, X. (2020). Applied Surface Science, 532, 147425.
Notes: Wang, N., Feng, Y., & Guo, X. (2020). Atomistic mechanisms study of the carbonation reaction of CaO for high-temperature CO2 capture. Applied Surface Science, 532, 147425.

## Slide 10: CO2 Adsorption and Desorption on Surfaces
10
SrO can react with H2O in flue gas to form Sr(OH)2.nH2O
CO2 adsorption first happens on the surface before CO2 diffuses into the bulk
SrO
Sr(OH)2
Sr(OH)2.8H2O
SrCO3
H2O
H2O
CO2
CO2
CO2
Sr(OH)2.1H2O
7H2O
CO2

## Slide 11: CO2 adsorption reaction pathways
11
Relative energies of CO2 capture reaction
Bicarbonate
carbonate
Carbonate

## Slide 12: CO2 reaction thermodynamics
12
where and are the DFT calculated electronic energy and zero-point vibrational energy.
The internal energy, , and the entropic terms includes vibrational, translational and rotational terms at the temperature T of interest.
Vibrational frequencies were done using the harmonic oscillator, ideal gas and rigid rotor approximations.

## Slide 13: Molecular Dynamics for ionic transport and solvation in electrolytes

## Slide 14
Zwitterionic Effect on
Ionic Solvation and Transport in Electrolytes
Manh Tien Nguyen
Qing Shao
Department of Chemical and Materials Engineering
University of Kentucky

## Slide 15
SHAWN L. MINTER/AP
http://www.youtube.com/user/ajgill206rr?feature=watch
Flammable liquid electrolytes have safety issues: leakage and short-circuit One solution: Develop solid-state electrolytes with high ionic conductivity
Challenge: Need to enhance Li+, Na+ and K+ kinetics/diffusion in solid-state electrolytes
Zhang et al. Science advances 5.5 (2019)
Li+ battery is critical for sustainable future
Na+ and K+ are alternatives to Li+ batteries due to their abundance and low-cost﻿
Safer batteries with solid-state electrolytes
https://www.targray.com/li-ion-battery/electrolyte

## Slide 16
S
H
N
N
C
O
Zwitterion (ZW)
Li+
Anion-
ZW+
ZW-
ZW molecules possess both cationic and anionic groups
They can associate with both Li+ and anion and themselves
We can leverage this ability to increase ionic conductivity of solid polymer electrolytes
Zwitterionic Electrolytes

## Slide 17
Jones et al. ACS central science 8.2 (2022)
Zwitterionic Electrolytes
Poly(ZW) scaffold can enhance the target ion transport

## Slide 18
O
N
P
O
C
N
N
F
O
C
S
N
MPC
2-methacryloyloxyethyl phosphorylcholine
SB
sulfobetaine ethylimidazole
CB
carboxybetaine ethylimidazole
EO10
(ethylene oxide)10
TFSI-
bis(trifluoromethylsulfonyl)-imide
3 ZW Structures
S
H
N
N
O
Molecular Dynamics Simulation
Na+
K+
Li+

## Slide 19
ZW free Li+ from trapping effect of poly(ethylene oxide)
ZW could also trap Li+ and slow down its transport
Ionic Dissociation Effect of ZW in PEO

## Slide 20
ZW structures and surface charge density
A sigma profile is the probability distribution of a molecular surface segment having a specific charge density
The electronegativity of a molecule can be quantified by the area of σ>=0.01 e/Å2 region
Charge density:
    CB > MPC > SB
Electronegativity:
    MPC > SB >CB
MPC (-PO4)
SB (-SO3)
CB (-CO2)

## Slide 21
Percentage of cations not associating with EO10
MPC > CB > SB in releasing cations from association with EO10
The effect MPC is weakened from Li+ to K+
ZW Dissociation Effect
MPC (-PO4)
SB (-SO3)
CB (-CO2)
EO10
Na+
K+
Li+

## Slide 22
All ZW slow down cationic diffusions of K+ while only SB does for Li+ and Na+
ZW can have the dissociation effect without reducing diffusion for Li+ and Na+
Ratios of cationic diffusion coefficients: With vs without ZW
ZW Effect on Cationic Diffusion

## Slide 23: Deep Learning Potential For Investigation of Chemical Conversion of CO2 at Air-Reactive Deep Eutectic Solvent Interface
Manh Tien Nguyen (Tien)
Mentors: Qing Shao*, Yueh-Lin Lee** & Yuhua Duan**
*University of Kentucky
**National Energy Technology Lab
Notes: #1: Hello everyone. My name is Tien. I’m a phd candidate from University of Kentucky. Today I’m presenting my internship project at NETL under the mentorship of Dr. yuehlin Lee and Dr. yuhua Duan.
The project is about “Quantum computing of vibrational properties for CO2 capture application

## Slide 24
Dmitry Kovalchuk/Shutterstock.com
Deep Eutectic Solvents for CO2 Capture
Carbon capture is necessary to reduce CO2 emissions from burning fossil fuels, which has led to global warming
Traditional CO2 capture by aqueous amine has drawbacks such as high energy consumption, equipment corrosion, and toxic leakage to the environment.
Deep eutectic solvents (DESs) are promising due to their low vapor pressure, low corrosion, non- toxicity, relatively low cost, and biodegradable nature.
Notes: #5: CO2 is captured by reactions with amine-based solventto reduce emission from burning fosil fuels and help solve the grobal warming. to simplify the calculation, We use NH3 as model solvent. The reaction is as followed: NH3 reacts to CO2 resulting in NH2COOH.

## Slide 25
Reactive DES can capture CO2 at low partial pressure (410ppm)
Reactive DES for Direct Air Capture
CNP: 2-cyanopyrrolide
EMI: 1-ethyl-3-methylimidazolium
CNPC
EG: ethylene glycol
EMIC
EGC
CNPC: carbamate
EMIC: carboxylate
EGC: carbonate
Product Distribution
Lee et al. ACS Sustainable Chemistry and Engineering. 2021, 9(3), 1090-1098

## Slide 26
Machine Learning Potential
Friederich, Pascal, et al. "Machine-learned potentials for next-generation matter simulations." Nature Materials 20.6 (2021): 750-761.
Machine learning potentials allow simulation of complex CO2 capture reactions at solvent-air interface with solvation effect

## Slide 27
Deep Learning Potential Development
DPMD simulations
Construct database
Train and validate model
27

## Slide 28
[EMI][CNP]:EG = 1:2 (6 EMI, 6 CNP and 12 EG molecules)
Adding 1, 5, and 10 CO2 molecules, 1, 5 reaction products (CNPC, EMIC, EGC)
Interface: ~2x2x2 nm slab of DES with 2 nm thick vacuum on both sides.
Construct Database
Classical molecular dynamics using OPLS-AA force field to generate initial configurations
Ab-initio simulations at 300-1000K and well-tempered meta-dynamics to collect more configurations
Get potential energy and atomic forces for collected structures at DFT level of theory ﻿(molopt-DZVP basis set and GTH pseudopotential)
Bulk
Interface
Initial configurations

## Slide 29
Atomic environment descriptor: 8 Å radius, smooth-edition, angular-radial descriptors
DP neural networks: 3 layers of 600x600x600 ﻿neurons.
DP model with the best performance will be selected to run DPMD simulations.
Train and Validate Deep Potential Model
z
Energy
Force
Active Learning Scheme
29
Xu, Nan, et al. The Journal of Physical Chemistry C124.30 (2020): 16278-16288.

## Slide 30
Dataset size | Bulk | Interface
Initial configs from MD and AIMD | 17310 | 5157
Active learning explored | 18893 | 13139
Optimize weights and biases by ﻿the stochastic gradient descent method for minimizing atomic energy and force ﻿errors.
Final model with energy error of 2 meV/atom and force error of 0.3 eV/Å
500k iteration step can reduce force error to ~0.1 eV/Å
30
Train and Validate Deep Potential Model
Force and energy errors after 100k steps

## Slide 31
Run well-tempered metadynamics simulations with the Deep Potential at 300K.
The free energy surfaces (FESs) are constructed for the bonding distance of CO2 and three DES components: CNPC, EMIC and EGC
31
Deep Potential Molecular Dynamics
Bulk
Interface
CNPC
EMIC
EGC

## Slide 32
Proton transfer observations
32
Deep Potential Molecular Dynamics
From EG to EG
From EG to CNP

## Slide 33
33
CNPC
Deep Potential Molecular Dynamics
EGC
EMIC

## Slide 34
34
Free Energy Surface
Deep Potential Molecular Dynamics
In Bulk
In Interface
CNP-CO2 has the lowest stability: the least product yield
The energy barrier: EMI-CO2 > EG-CO2 : EGC is the most yielded product
EGC is more stable in bulk than in the interface while EMIC is the opposite

## Slide 35
For advanced real-time monitoring and control of gas species in combustion environments, development of efficient sensing platforms and new sensor materials able to work under harsh environments are required.
Semiconducting optical-based sensor platforms show promise. MOx metal-oxides and ABO3 perovskite-oxides can be attractive for high-temperature applications due to their high decomposition temperatures and structural stability; ABO3 allows tunable electronic and optical properties owing to flexible choices of A, B dopants and forming oxygen non-stoichiometric point-defects
ML pipeline for perovskites materials discovery
Machine learning (ML) approach from first-principles modeling to calculate band gap in addition to extreme gradient (XG) boosting regression to predict perovskite conductivity with the intention to generate sensor candidates.

## Slide 36
ML-driven discovery pipeline
Exploring the vast compositional space of ABO₃ perovskites by selecting 1-2 elements from 13 options for the A-site and 1-2 elements from 36 options for the B-site, creating around 187 million initial combinations.
A site | Ba | Bi | Ca | Ce | Gd | La | Mg | Nd | Pr | Sm | Sr | Y | Yb
B site | Al | Be | Ca | Ce | Co | Cr | Cu | Dy | Er | Fe | Ga | Gd | Hf
 | In | La | Lu | Mg | Mn | Mo | Nb | Nd | Ni | Pr | Sc | Si | Sm
 | Sn | Tb | Th | Ti | V | W | Y | Yb | Zn | Zr |  |  | 
Initial Compositions
Stability Prediction
Conductivity Prediction
Ranking Top Materials
Web Tool
ML Pipeline

## Slide 37
Predicting perovskite stability
A gradient boosting classification model was employed for predicting perovskite stability.
The model achieved a Mean F1 score of 0.95 ± 0.02 on 5-fold cross-validation, indicating high accuracy.
The model leverages site-specific elemental features, including cation-oxygen bond distance, Mendeleev number, oxidation states, and ionic radius
The machine learning model was trained using experimental data obtained from the ICSD database and published literature.
~187 millions ABO3
~39 millions
This stability prediction step reduced the initial ~187 million combinations to approximately 39 million stable perovskite candidates
Zhai, X., Ding, F., Zhao, Z., Santomauro, A., Luo, F. and Tong, J., 2022. Predicting the formation of fractionally doped perovskite oxides by a function-confined machine learning method. Communications Materials, 3(1), p.42.

## Slide 38
High-Throughput Conductivity Prediction
An XGBoost regression model was developed for predicting conductivity
The model has high prediction accuracy, with an R² value of 0.99 and an RMSE of 0.18
The XGBoost model was trained on the datasets reported by Priya et al.
A feature database comprising ~39 million perovskite candidates was constructed. This database incorporates 100 features derived from the Materials Project database (for constituent oxides) and Shannon tables (for elemental properties)
The model predicts conductivity profiles across a wide range of temperatures (300-1000°C) and oxygen pressures (10⁻²⁰ to 1 atm).
Priya, Pikee, and Narayana R. Aluru. "Accelerated design and discovery of perovskites with high conductivity for energy applications through machine learning." npj Computational Materials 7, no. 1 (2021): 90.
Notes: Modified XGB model hyperparameters to avoid overfitting:
Original: n_estimators=150,max_depth=40
Modified: n_estimators=600, max_depth=10, learning_rate=0.05, subsample=0.8, colsample_bytree=0.8

## Slide 39: XG Boost Regression
highest 10 importance out of 112 features
Importance (%) | Feature | Description
56.05683 | EN_B_MIN | Minimum electronegativity of the B site atoms including M site (dopants) atoms
8.888567 | IR_B_AVG | Average ionic radius of A site atoms including M site (dopants) atoms
6.662896 | RO_B_MIN | Minimum density of the B site oxides (Materials Project) including M site oxides
6.381965 | EN_B_MAX | Maximum electronegativity of B site atoms including M site (dopants) atoms
2.961624 | CV_B_AVG | Average cell volumes of B site oxides including M site oxides
2.689203 | AM_B_AVG | Average atomic mass of B site atoms including the M (dopants)
2.166945 | BM_A_MAX | Maximum bulk modulus of A site oxides (Materials Project) including M site oxides
2.00186 | POL_B_MAX | Maximum polarizability of B site atoms including M site (dopants) atoms
1.933203 | CV_B_MIN | Minimum cell volume of the B site oxides (Materials Project) including M site oxides
1.801741 | MM_B_DIF | Difference of maximum & minimum magnetic moment of the A site oxides (Materials Project) including M site oxides
91.54 |  | 
RMSE of validation data = 0.246
R2 of validation data = 0.986
TEMP importance = 0.0149 = rank 55
PO2 importance = 0.00838 = rank 68
  7,230 experiment conductivity data points across 415 unique compositions

## Slide 40
Ranking top O₂ sensing materials
Perovskites are ranked based on their O₂-conductivity gradients
Top-performing materials are validated against available literature to confirm the model's predictions.
The analysis identified top-performing candidates exhibiting significant conductivity changes (3 orders of magnitude) across the full range of O₂ partial pressures
# | Composition | pO2 (%) | Temp (oC) | ∆log10(Conductivity) | Experimental reported
1 | La0.4,Sr0.4 TiO3 | 1e-18 - 100 | 930 | 3.0789201 | La0.4Sr0.4 TiO3
2 | La0.6Sr0.1TiO3 | 1e-18 - 100 | 930 | 2.9785082 | 
3 | La0.45Sr0.25 TiO3 | 1e-18 - 100 | 930 | 2.924773 | 
4 | La0.55Sr0.15TiO3 | 1e-18 - 100 | 930 | 2.9047394 | 
5 | La0.5Sr0.2TiO3 | 1e-18 - 100 | 930 | 2.887693 | 
6 | La0.3Sr0.5TiO3 | 1e-18 - 100 | 930 | 2.7824388 | 
7 | Ba0.25Y0.45TiO3 | 1e-18 - 100 | 930 | 2.7820268 | 
8 | La0.4Sr0.3Nb0.05Ti0.95O3 | 1e-18 - 100 | 930 | 2.7802086 | 
9 | Ba0.25Y0.45Nb0.05Ti0.95O3 | 1e-18 - 100 | 930 | 2.7801607 | 
10 | La0.25Sr0.55Nb0.05Ti0.95O3 | 1e-18 - 100 | 930 | 2.7787879 | 

## Slide 41
Interactive Web Tool
An interactive web tool has been developed to enable researchers to leverage the predictive power of the ML model
The web tool allows users to input perovskite compositions and obtain ranking of promising candidates with conductivity profiles, and O₂-conductivity gradients

## Slide 42
Interactive Web Tool
Output of the web tool: